SOUTH DAKOTA SCHOOL OF MINES AND TECHNOLOGY

DEPARTMENT OF METALLURGICAL ENGINEERING

MET 320	QUIZ 4b	Dec. 11, 1998

1.	Pure, liquid Cu2O at 1423 K is to undergo electrolysis to form O2 gas at a pressure of 1 ATM and pure liquid Cu.  What cell potential is needed? (15)

2.	Calculate the cell potential if the O2 pressure is 1.2 ATM, the oxide is dissolved in a more stable second oxide in which the activity of Cu2O (relative to pure, liquid oxide) is 0.4, and the produced liquid Cu is collected in a liquid Ag-Cu alloy in which the mole fraction of Cu is 0.2.  Activity data for liquid Ag-Cu alloys at 1423 K are given below. (10)

DATA:

2 Cu(l) + 0.5 O2(g)  =  Cu2O(s)     	∆G°= -195,000 -7.12TlnT +143T Joules/gmole

Cu2O(s) = Cu2O(l) 		∆G°= 13,580 – 9.0 T Joules/gmole

Activity data for liquid			F = 96,525 Joule/volt

Ag-Cu Alloys at 1423 K

XCu 	aCu

0.0	0.000

0.1	0.260

0.2	0.422

0.3	0.535

0.4	0.616

0.5	0.679

0.6	0.731

0.7	0.782

0.8	0.841

0.9	0.912

1.0	1.000