South Dakota School of Mines and Technology

Department of Materials and Metallurgical Engineering

MET 320	HQ 3	Nov 8, 2000

- Write the Fundamental Equations for a closed system.

2.	Find the adiabatic flame temperature for the combustion of C2H2. With an oxygen-nitrogen mixture which is 50% O2 and 50% N2.  The mixture starts at a temperature of 1000 K and the C2H2 starts at minus 23 °C.  Use the data provided below only.  DRAW A CALCULATION SCHEMATIC.

C2H2 (g)+ 2.5O2(g) = 2CO2 (g) + H2O(g)

Species	Heats of Formation	Cp

(Calories/g mole at 298°K)	(cal/ gmole °K)

C2H2(g)	54,190	19.0

H2O(g)	-57,800	10.5

CO2(g)	-94,000	13.6

O2(g)		8.6

N2(g)		7.0

3.	Using the attached JANAF Tables determine ∆H° K for the reaction below at 1300 K.

Cu(sol) + F2 (gas) =  CuF2(liq).

- Two Parts:

- Use the JANAF Tables to determine the amount of heat it would take to raise one gram mole of pure solid Cu at 500 K to gaseous Cu at 3000 K.

b)	Draw a calculation schematic for the above computation assuming the only data available are heat capacities and heats of transformations.