SOUTH DAKOTA SCHOOL OF MINES AND TECHNOLOGY

DEPARTMENT OF METALLURGICAL ENGINEERING

MET 320	HQ 4	Dec. 4, 2001

- Show on the attached Ellingham Diagram

- the pressure of O2 in equilibrium with Si and SiO2 at 1500°C

- the H2/H2O ratio in equilibrium with Mn and MnO at 1500°C

- What is the volume of one mole of CO2 at its critical pressure and temperature?

- Set up a reaction extent problem for

3H2 + N2 = 2 NH3

if there are three moles of each of the reactants initially and no ammonia.  The KEQ is 1.5  and the total pressure is 8 atm.

- Calculate the Gibbs energy change for the oxidation of liquid copper in a liquid Ag-Cu alloy at a mole fraction of 0.1 with O2 at a pressure of 2x10-4 ATM to form a liquid oxide with an activity of Cu2O (relative to pure, liquid oxide) of 0.4.   The temperature is 1423 K.  Use only the Data below.

2 Cu(l) + 0.5 O2(g)  =  Cu2O(s)     	G°= -195,000 -7.12TlnT +143T Joules/gmole

Cu2O(s) = Cu2O(l) 		G°= 13,580 – 9.0 T Joules/gmole

Copper Activities in Liquid 	Ag-Cu Alloys at 1423 K

Xcu		0	0.1	0.2	0.3	0.4	0.5	0.6	0.7	0.8	0.9

aCu		0	0.260	0.422	0.535	0.616	0.679	0.731	0.782	0.841	0.912

5.	Use the data given below for the liquid Cu-Sn system at 1400 K to determine the enthalpy change when (assume all components start in the liquid state at 1400 K)

a)	60 moles of Sn and 40 moles of Cu are mixed at 1400 K

b) 	2 moles of Sn are dissolved in a large quantity of Cu-Sn alloy having a mole fraction of Cu of 0.9.

## Heats of Mixing for Liquid Cu-Sn Alloys at 1400 K

XSn	0.1	0.2	0.3	0.4	0.5	0.6	0.7	0.8	0.9

(cal/mole)	-666	-979	-934	-715	-475	-264	-97	13	52

(cal/mole)	-5233	-1901	252	706	681	506	311	176	49