South Dakota School of Mines and Technology

### Department of Materials and Metallurgical Engineering

## Met 320	Final Exam	Dec. 18, 2001

Constants:

R = 1.987 cal/K•gmole = 8.31 J/K•gmole

F = 23,060 cal/volt•equivalent = 96,259 Joule/volt• equivalent

- Ten moles of ideal gas are compressed from 1 atm to 10 atm.  Find q, w, U, and S if the process occurred

  - Isothermally

  - Adiabatically

  - Isochorically

- Write the Fundamental Equations for a closed system.

- According to Table AV on the accompanying data sheet, Fe and Fe are in equilibrium at one atmosphere and 1187 K.  What would this equilibrium temperature be at 1000 atm?  The respective densities of alpha and gamma iron are 7.88 and 8.14 g/cm3 and the molecular weight of iron is 55.85.

- Show on the attached Ellingham Diagram

- the pressure of O2 in equilibrium with Ti and TiO2 at 1200°C

- the CO/CO2 ratio in equilibrium with Ti and TiO2 at 1200°C

- What cell potential would be required to produce Mg (l) and Cl2 (g) from MgCl2 (l) at 888 ºC ?  Assume the MgCl2 is pure, that the Mg has an activity relative to pure liquid Mg of 0.45, and that the pressure of the Cl2 is 0.3 atm.

- Use the data given below for the liquid Cu-Sn system at 1400 K to determine the enthalpy change when one mole of Sn is dissolved in a large quantity of Cu-Sn alloy having a mole fraction of Cu of 0.6. (assume all components start in the liquid state at 1400 K)

## Integral Molar Heats of Mixing for Liquid Cu-Sn Alloys at 1400 K

XSn	0.1	0.2	0.3	0.4	0.5	0.6	0.7	0.8	0.9

(cal/mole)	-666	-979	-934	-715	-475	-264	-97	13	52

7.	For the batch composition indicated by the “◘” on the attached CaO-SiO2 Al2O3 ternary phase diagram,

  - Short answer

    - What is the first crystal?

    - What are the final three crystals?

    - What is the temperature of last liquid?

  - Characterize the system at 1200 °C