South Dakota School of Mines and Technology

Department of Metallurgical Engineering

MET 320	HQ 3	Dec. 3, 2002

- Write the first four of the “Big Six Equations” relating pressure, fugacity, mole fraction, and activity to Gibbs energy.

- Ellingham Diagram: find

- The pressure of O2 in equilibrium with V and V2O3 at 1400°C. (Show work.)

Ans:

- The H2/H2O ratio in equilibrium with V and V2O3 at 1400°C. (Show work.)

Ans:

- Which of the following pure oxides could be reduced to pure metal by C at 1400°C?  Cr2O3,   MnO,   SiO2,   TiO2.

Ans:

- What is the melting point of Ca?  (Circle the location on the diagram.).

- Estimate the  of one mole of Mg(l).  (Show construction lines.)

Ans:

- What is the volume of one mole of O2 at its two times its critical pressure and 1.2 times its critical temperature?

- Set up a reaction extent problem for

SO2 + 0.5 O2 = SO3

if there are initially 10 moles of SO2, 5 moles of  O2, and one mole of SO3.  The KEQ is 1.19  and the total pressure is 2 atm.

5.	Use the data given below for the liquid Cu-Sn system at 1400 K to determine the enthalpy change when (assume all components start in the liquid state at 1400 K)

## Heats of Mixing for Liquid Cu-Sn Alloys at 1400 K

XSn	0.1	0.2	0.3	0.4	0.5	0.6	0.7	0.8	0.9

(cal/mole)	-666	-979	-934	-715	-475	-264	-97	13	52

- 10 moles of Cu are dissolved in a large quantity of Cu-Sn alloy having a mole fraction of Sn of 0.8.

- 2 moles of Sn and 8 moles of Cu are mixed at 1400 K

6.	Show how to find the Gibb’s Energy change and direction of the reaction

Pb(l) + SO2 + O2 = PbSO4(s)

when the pressure of SO2 is 0.1 atm, the pressure of O2 is 2 atm, the activity of Pb is 0.1 relative to pure liquid Pb, and the PbSO4 is pure solid.