South Dakota School of Mines and Technology

Department of Materials and Metallurgical Engineering

MET 320	HQ 4	Dec 11, 2003

Closed Book and Notes	No Calculators	Data Sheet Provided MET 320

R = 1.987 cal/K•gmole = 8.31 J/K•gmole

F = 23,060 cal/volt•gram equivalent = 96,259 cal/volt•gram equivalent

- Set up a reaction extent problem for

3H2 + N2 = 2 NH3  	         KEQ = 1.2                       PT = 5 atm

The table below shows the number of moles of each component initially.

| Species | Moles initially |  |  |
| --- | --- | --- | --- |
| NH3 | 2 |  |  |
| H2 | 1 |  |  |
| N2 | 1 |  |  |
| total | 4 |  |  |

# Use the attached Ellingham Diagram for the problems below.

# (Show your work and submit the Ellingham Diagram.)

- Show on the attached Ellingham Diagram

- The pressure of O2 in equilibrium with Ca and CaO at 1000°C

- The H2/H2O ratio in equilibrium with Si and SiO2 at 1000°C

- The value for Standard Gibbs Energy change for the formation of one mole of TiO2 at 1000 °C.

##### Refer to the data for the Al-Au system at the end of the exam for Problems 3 and 4

- Calculate the Gibbs energy change for the oxidation of liquid Al in a liquid Al-Au alloy at a mole fraction of 0.1 with O2 at a pressure of 1x10-12 ATM to form pure, solid Al2O3 oxide.   The temperature is 1338 K (1611 ºC).

2/3 Al(l)  +  O2(g) =  4/3 Al2O3 (s)     	 G°= -711,620 Joules/gmole O2

4.	How much heat would be expected from mixing

- 2 moles of liquid Al at 1338 K and 8 moles of liquid Au at 1338 K?

- 1 mole of liquid Al at 1338 K and 1,000,000 moles of liquid Al-Au alloy of XAl = 0.7 at 1338 K?

5.	What voltage would be needed to form pure, liquid Mg from a cell at 800 K from pure, liquid MgCl2 The pressure of Cl2 is 0.1 atm?

MgCl2(l) = Cl2(g) + Mg(l)	G°= 605,000 -125.4T  J/gmole

6.  Fill in the blank.

| To obtain in a binary alloy | Given | Use Method or Equation |
| --- | --- | --- |
| The Integral Molar Quantity | The Partial Molar Quantities |  |
| The Partial Molar Quantity #1 | The Partial Molar Quantity #2 |  |
| Both Partial Molar Quantities | The Integral Molar Quantity |  |

DATA from Hultgren, et al.  All G and H data are in calories.  All S data are in calories/K

# Text boxes

0.0000035