South Dakota School of Mines and Technology

Department of Materials and Metallurgical Engineering

MET 320	HQ 2	Nov. 10, 2008

1.	What is the configurational entropy change for the mixing of 2 gram moles of argon with 8 gram moles of neon?

2.	Write the

a) 	Remaining three Fundamental Equations for a closed system:

dU = TdS – PdV

dH = U + PV =

dA = U – TS =

dG =

- Other Thermodynamic Relations obtained from dU = TdS – PdV

- Maxwell Relation obtained from dU = TdS – PdV

- Definition of Chemical Potential,

- Show how to calculate a good estimate of the boiling temperature of gold from the following data:

4.	Find the adiabatic flame temperature (AFT) for the combustion of C2H2 with air (21% O2 and 79% N2).  The air starts at 800 K and the C2H2 start at 298 K.  Use the data provided below only.  Half the credit for this problem depends on a correct calculation schematic.

C2H2 (g)+ 2.5O2(g) = 2CO2 (g) + H2O(g)

Species	Heats of Formation	Cp

(J/g mole at 298°K)	(J/ gmole °K)

C2H2(g)	226,800	80

H2O(g)	-241,200	44

CO2(g)	-393,500	57

O2(g)		36

N2(g)		29