South Dakota School of Mines and Technology

Department of Materials and Metallurgical Engineering

MET 320	HQ 3	Dec. 11, 2008

Faraday’s Constant is 96,525 J/eq/volt

- Use the Ellingham Diagram to find (Show your work on the Diagram)

- The pressure of O2 in equilibrium with Si and SiO2 at 1400°C.

Ans:

- The H2/H2O ratio in equilibrium with Si and SiO2 at 1400°C.

Ans:

- Which of the following pure oxides could be reduced to pure metal by Si at 1400°C?  Cr2O3,   MnO,   Al2O3,    TiO2.

Ans:

- What is the melting point of Mg?

Ans:

- Estimate the  of one mole of Mg(l).

Ans:

- What is the volume of one mole of O2 at 100 atm and 1.2 times its critical temperature?

- Short Answer:

  - What is the relative partial molar heat of mixing for an Ideal solution?

  - Describe in words the difference between G and Gº?

  - Write the missing term for the first four of the “Big Six Equations”:

i)   IG  	  _____

ii)  RG	   _____

iii) ISoln  _____

iv) RSoln  _____

4.	Set up a reaction extent problem for

2 NH3   =  3H2 + N2      KEQ = 4.2                       PT = 3 atm

The table below shows the number of moles of each component initially.

| Species | Moles initially |  |  |
| --- | --- | --- | --- |
| NH3 | 13 |  |  |
| H2 | 2 |  |  |
| N2 | 5 |  |  |
| total | 20 |  |  |

5.	Use the data given below for the liquid Au-Ge system at 1400 K to determine the enthalpy change when (assume all components start in the liquid state at 1400 K)

## Heats of Mixing for Liquid Au-Ge Alloys at 1400 K in cal/gmole

XAu	0.0	0.1	0.2	0.3	0.4	0.5	0.6	0.7	0.8	0.9	1.0

-1950	-2260	-2570	-2820	-3010	-2090	-1340	-750	-330	-80	0

0	20	70	150	250	-480	-1400	-2470	-3710	-5110	-6690

- Five gmoles of Ge are dissolved in a large quantity of Au-Ge alloy having a mole fraction of Au of 0.6.

- Three gmoles of Au and 7 gmoles of Ge are mixed.

6.	What voltage would be needed to form pure, liquid Mg from a cell at 1000 K from pure, liquid MgCl2.  The pressure of Cl2 is 0.1 atm?

MgCl2(L) = Cl2(G) + Mg(L)	            G°= 605,000 -125.4T  J/gmole

Scratch Sheet

Please discard before submitting the exam.