South Dakota School of Mines and Technology

Department of Materials and Metallurgical Engineering

MET 320	HQ 3	Oct 17, 2011

Closed Book and Notes	No Calculators	Data Sheet Provided MET 320

No questions are answered during the exam.  If there seems to be an error in the question, state a reasonable correction and proceed with the solution.

R = 1.987 cal/K•gmole = 8.31 J/K•gmole

1. 	Write the

a. Fundamental Equations

dU = TdS – PdV

dH =

dA =

dG =

b. The Maxwell Relations that comes from dU = TdS - PdV

c. The so-called “Other Thermodynamic Relationships” that comes from dU = TdS - PdV

2. 	What is the entropy change for the ideal mixing of 40 moles of Helium with 60 moles of Argon?

3.	What is the

- Criterion of equilibrium for a system at constant T and V?

- Criterion of equilibrium for a system at constant T and P?

- The starting point for deriving the Clausius Equation?

- The definition of chemical potential?

- The Gibbs-Helmholtz Equation?

4. 	All the reactants and products in the following reaction are in their most stable form at 298 K.

3 Mn + Cr2O3   = 3 MnO + 2 Cr

Calculate at 298 K the

a) Enthalpy of reaction and

b) Entropy of reaction

5. 	Draw a calculation schematic by which you could determine the AFT (adiabatic flame temperature) for the combustion of one gmole of C (graphite) starting at 298 K with oxygen at 700 K to form CO2. Show how to calculate each enthalpy change and give the appropriate values for the required parameters from the data sheet. No computations or integrations are required – just the schematic with T labels.

6. 	Show how to calculate the heat of vaporization of Mg from the following data: the vapor pressure at the melting point (922K) of 4.08 x 10-3 atm and its boiling point (p = 1 atm) is 1363K.

Scratch Paper - discard