SOUTH DAKOTA SCHOOL OF MINES AND TECHNOLOGY

DEPARTMENT OF METALLURGICAL ENGINEERING

MET 320	Short Exam 4a	Dec. 5, 2012

Closed Book No Calculators No Notes

Data Sheet Provided

Constants:

R = 1.987 cal/K•gmole = 8.31 J/K•gmole

F  = 96,525 Joule/(volt*Equivalent)

- How many moles of NH3 would be present at equilibrium in a system at 10 atm that initially contained 

1mole of H2, 
5 moles of N2, and 
12 moles of NH3 ?

The temperature is such that the equilibrium constant for the reaction below is as stated.

3H2(g) +  N2(g) = 2NH3(g)        K = 3.2

Work ONE of the following two problems.

- Which direction will the following reaction proceed at 800 K when the activity of Mg relative to pure, liquid Mg is 1.0?  The activity of MgCl2 is 0.1 relative to pure, liquid MgCl2; and the pressure of Cl2 is 2x10-5 atm.

MgCl2(l) = Cl2(g) + Mg(l)

- The goal is to make a liquid Ag-Cu alloy at 1423 K into pure Ag by reacting the copper in the alloy with the oxygen in air (21% O2) at 1 atm to form liquid, cuprous oxide Cu2O dissolved in a molten oxide layer floating on the alloy as shown.  The activity of the cuprous oxide in the oxide covering is 0.7 relative to pure, liquid cuprous oxide.

DATA:

2 Cu(l) + 0.5 O2(g)  =  Cu2O(l)     	∆G°= -181,420 -7.12TlnT +134T       Joules/gmole

Activity data for liquid

Ag-Cu Alloys at 1423 K

xCu 	aCu

0.0	0.000

0.1	0.260

0.2	0.422

0.3	0.535

0.4	0.616

0.5	0.679

0.6	0.731

0.7	0.782

0.8	0.841

0.9	0.912

1.0	1.000 							1423 K

I am working problem ______.

Extra paper (use as needed)

Scratch Paper - discard

# Text boxes

Molten Oxides including Cu2O

Molten Ag + Cu

Air