South Dakota School of Mines and Technology

Department of Materials and Metallurgical Engineering

MET 422	HQ 3	Dec 4, 2002

MI 222	(open book)	11:00 AM

- What is the value of the heat transfer coefficient for a 1 cm diameter sphere falling in air at 20 m/sec?  (You may use data from Problem #2 if you wish.)

2.	A steel specimen 8x8x40 cm at room temperature is suspended in a hot furnace at 825 °C.  Determine the temperature at the mass center of the specimen after 4 minutes.  Use ONLY the following data for your computations, if possible.

h	=	200 	Wm-2K-1	steel	=	7,900 	Kg m-3

ksteel	=	40 	W m-1K-1	kair	=	0.04 	W m-1K-1

Cpsteel	=	504 	J Kg-1K-1	Cpair	=	1000 	J Kg-1K-1

Prair	=	0.7		MWair	=	28.8

Derive (or reduce from the Equations of Change) the partial differential equation for two-dimensional heat transfer in a solid.  Assume no generation term.  Show all your work deriving it or the eliminations from the General Equation of Change.   T = f(t, x, y)

- A composite wall is composed of the materials given in the table below.  Also given is each material’s thickness and thermal conductivity.  How many kilowatts would be lost through such a wall if it has an area of 10 m2 and an air temperature differential across it of 1000 degrees C?  The heat transfer coefficient on both sides is 20 Wm-2K-1.

| Table 1. Composite wall data |
| --- |
| Material | Thickness, m | k , W m-1 K-1 |
| Chrome Brick | 0.10 | 2.0 |
| Fire Brick | 0.20 | 1.0 |
| Insulating Brick | 0.40 | 0.5 |