SOUTH DAKOTA SCHOOL OF MINES AND TECHNOLOGY

DEPARTMENT OF MATERIALS and METALLURGICAL ENGINEERING

MET 426	HQ 1	Feb 11, 2000

1.	Find ∆G° at 1873 K for the change in standard state for the reaction.

Mn(l)	=	Mn(1 wt % in Fe)

MW Mn	=	54.9

MW Fe	=	55.9

	=	1.33

- What is the slope of a line on the Ellingham diagram (RTLog PO2, Kcal vs T) for the reaction

2C + O2 = 2 CO

when the percent carbon is

- 1 wt %.

- 0.1 wt %

Assume that fC = 1.

Data:

C(gr) + 0.5O2 = CO		G0 = -111,700 –87.65T  Joules/gfw

C(gr) = C 			G0 = 22,7594 –42.26T  Joules/gfw

3.	What is the mathematical relationship between the slope on a Darken Plot* () at infinite dilution and the Interaction Coefficient, .

* ln vs. (1-xi)2

4.	Write a short paragraph on 1) the reason for using 1 wt % standard state and 2) the graphical relationship between ai and hi .  Use a figure of ai  vs xi .