Department of Materials and Metallurgical Engineering

South Dakota School of Mines and Technology

Met 426/526	HQ3a	May 1, 2000

- A steel melt at 1600 C is covered with a slag of basicity 0f 2.5with 3 wt% MnO, and 4 wt% FeO.  What is the wt% Mn in the steel?

- How is the reference pressure of oxygen fixed in a steelmaking oxygen probe?