Department of Materials and Metallurgical Engineering

South Dakota School of Mines and Technology

Met 426/526	HQ3b	May 3, 2000

- A 1040 steel melt at 1600 C is in equilibrium with CO gas at 1 atm.  What is the [% O].

- Assume a 100 ton steel melt at 1600 C has a [% O] = 0.002 and is covered with 4 tons of slag containing 20 wt% CaO, 10 wt% MgO 3, wt% MnO, and 4 wt% FeO.  What is the [% P] in the steel if the initial [%P] in the steel before the slag addition was 0.05 wt%.