TURN THIS SHEET IN ON TOP OF YOUR WORK

South Dakota School of Mines and Technology

# Department of Metallurgical and Materials Engineering

## Met 426/526	 HQ 1	Feb 23, 2006

1.	Sketch an iron blast furnace and label eight (8) parts of it.

- Use the attached data for the solid Fe-V system at 1600 K to find the standard Gibb’s Energy Change for pure, solid V at 1600 K going to V behaving as the infinitely dilute solution at 1 wt % in solid Fe at 1600 K.

- The equation for the line on the Darken Plot near infinite dilution for the Fe-V system at 1600 K is [0.7207(1-XV)2 + 0.0893].  Show how this could be used to find the interaction coefficient for V on V.

- Show the mathematical basis for determining the above Gibb’s Energy change as a function of temperature.

- Use the attached Ellingham Diagram to find

a)	The CO/CO2 in equilibrium with Fe and FeO at 800 C.

b)	The Standard Gibbs Energy change at 1873 K for the reaction

C (graphite) + CO2 (g) = 2CO (g)

- The equilibrium constant at 1600 C for the reaction

Si (l) + O2 (g) = SiO2 (s)

Ref: Hultgren, P. Desai, D. Hawkins, M. Gleiser, K. Kelley, Selected Values of the Thermodynamic Properties of Binary Alloys, ASM, 1973

Data:

C + 0 = C0(g)		K1600 =500

Si + 20 = Si02(s)		K1600=3.5 x 104

Activities of Si, 0, and C, in %, fC, fO, fSi all unity.

Molecular Weights: Fe = 55.85, V = 50.94