MET 426/526 (3-0)

Steel Making

- Students will know annual production tonnage rates for pellets, scrap, hot metal, and minimill products.

- Students will be able to convert to and perform calculations using the 1 wt% standard state.

- Students will be able to relate the interaction coefficient to the slope of the Darken Quadratic Formalism plot at infinite dilution.

- Students will be able to use interaction coefficients to determine the effect of dilute components on steel melt Equilibria.

- Students will be able to describe the fundamental ionic, viscosity, bonding, and composition differences between acid and basic slags.

- Students will be able to compute the relative effectiveness of deoxidation by sparging, vacuum degassing, and deoxidation additions.

- Students will be able to compute the effect of sparging on steel melt chemistry

- Students will be able to identify the required information about slag chemistry to calculate steel melt equilibria.

- Students will be able to construct simple spreadsheet models for the continuous casting of steel.

- Students will be able to describe in detail two DRI processes

- Students will be able to describe the fundamentals of the AOD process

- Students will be able to describe the fundamentals of ladle metallurgy