South Dakota School of Mines and Technology

Department of Materials and Metallurgical Engineering

Met 426/526	Homework

- Plot the activity of C in austenite relative to pure solid graphite as a function of both mole fraction and wt % C.  (To do this in Excel, one must make the mole fraction and the wt % the vertical scale and activity the horizontal scale.)

- Compute for each mole fraction for which activity data is tabulated in Hultgren, et al. the corresponding value of fC and wt % C.  Place the results in the table below.

| Selected Solution Values for C in Austenite at 1426 K |
| --- |
| xC | wt % C | aC | C | hC | fC | eCC |
| 0.00 0.01 0.02 0.03 0.04 0.05 0.06 0.07 0.08 0.09* |  | 0.000 0.053 0.116 0.190 0.276 0.378 (±0.028) 0.499 0.638 0.805 1.000 | 4.894 5.323 5.800 6.323 6.911 7.570 (±0.570) 8.309 9.121 10.064 11.111 |  |  |  |

*Phase boundary

- Construct a plot of hC vs. wt %C.

- Why is fC>1 when C>1?   [Normally, when i>1, fi<1; when i<1, fi>1 and when i=1, fi=1.]

- Estimate the value of the self-interaction coefficient of carbon.

Selected Thermodynamic Values for C Component in -Fe at 1426 K

C= C (in alloy)

| xC | aC | C | GMC | GXSC | HMC | SMC | Sxs |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.00 0.01 0.02 0.03 0.04 0.05 0.06 0.07 0.08 0.09* | 0.000 0.053 0.116 0.190 0.276 0.378 (±0.028) 0.499 0.638 0.805 1.000 | 4.894 5.323 5.800 6.323 6.911 7.570 (±0.570) 8.309 9.121 10.064 11.111 | -8312 -6105 -4710 -3643 -2753 (±200) -1973 -1267 -614 0 | 4500 4738 4981 5226 5478 5736 (±200) 6000 6268 6543 6823 | 10552 10729 10910 11094 11282 11474 (±500) 11671 11871 12076 12285 | 13.353 11.932 11.083 10.466 9.977 (±0.380) 9.568 9.213 8.899 8.615 | 4.244 4.201 4.158 4.115 4.070 4.024 (±0.380 3.977 3.929 3.880 3.830 |

*Phase boundary

Source -	Ralph Hultgren, Pramod Desai, Donald Hawkins, Molly Gleiser, and Kenneth Kelley:

Selected Values of Thermodynamic Properties of Binary Alloys, ASM, Metal Park, OH, 1973.