South Dakota School of Mines and Technology

Department of Materials and Metallurgical Engineering

Met 426/526	Homework 08

- Plot the activity of Si vs mole fraction of Si from 0 to 2 wt % Si in the liquid Fe-Si system at 1873 K.  Use (and include) a Darken Plot to accurately fix the curve.

- Derive an equation relating the interaction coefficient of a dilute component to the slope of the Darken Plot for that component at infinite dilution.