South Dakota School of Mines and Technology

Department of Materials and Metallurgical Engineering

Met 426/526	Homework

- Plot the activity of Si vs. mole fraction of Si in the liquid Fe-Si system at 1873 K.

- Plot the activity of Si vs mole fraction of Si from 0 to 2 wt % Si in the liquid Fe-Si system at 1873 K.  Use (and include) a Darken Plot to accurately fix the curve.

- Show the 1 wt % Si standard state in an expanded portion of the plot in problem 2.

- Derive an equation relating the interaction coefficient of a dilute component to the slope of the Darken Plot for that component at infinite dilution.

Note 1: 	wt% i 	= 	100xi*MWi/(xi*MWi+(1-xi)*MWFe)

( 	100xi*MWi/(0+xi*MWFe)

wt% i 	( 100[MWi/MWFe] xi

Note 2: 	b(1-xi)2 	= b-2bxi + xi2

( b-2bxi  		if xi is small.

For your calculation of the interaction Coefficient of Si on itself you will need the following data:

At 1873 K Hultgren at al. report for the liquid Fe-Si system

XSi    Activity Coefficient of Si

0.0	0.00132

0.1	0.00297

0.2	0.00950

0.3	0.0406

0.4	0.178

0.5	0.446

0.6	0.677

0.7	0.830

0.8	0.928

0.9	0.983

1.0	1.000