South Dakota School of Mines and Technology

Department of Materials and Metallurgical Engineering

Met 426/526	Homework

1.	Determine G° at 1600°C for the

Si + O2 = SiO2

For the following combinations of standard states:

Combination	Si	 O2	SiO2

1	pure l	1 atm	pure l

2	"	"	pure  cristobalite, high

3	 "	1 torr	pure l

4	 "	"	pure  cristobalite, high

5	1wt %	1 atm	pure l

6	 "	"	pure  cristobalite, high

7	"	1 torr	pure l

8	 "	 "	pure  cristobalite, high

DATA:

Si(l) + 02(g) = Si02 (B-cristobalite ,high)	G= - 218,600 + 47.40 T cal/gmole

Si(l) in iron;	1873°K = 0.00132*		log fSi = 0.07 [% Si]*

ATOMIC W Si = 28.09	H°fusion, (B-cristobalite ,high)= 2,290 cal/gmole

Tfusion,(B-cristobalite ,high) = 1,996 K

2.	In the design of a high-temperature calorimeter employing molten 	iron at 1600°C the feasibility of using a quartz crucible has been considered.  However, the extent of the solution of the crucible into the iron must be ascertained in as much as contamination of the molten iron by silicon cannot be tolerated to an extent greater than 0.5%. To prevent oxidation of the iron melt the calorimeter is filled with purified argon for which

P02(g) = 10-10 atm.	Calculate the %Si in the iron, resulting from solution of the crucible.

Si(l) + 02(g) = Si02 (B-quartz)	G= - 218,600 + 47.40 T

Si(l) in iron;	1873°K = 0.00132*		log fSi = 0.07 [% Si]*

* Data obtained from Hultgren et al.