South Dakota School of Mines and Technology

Department of Materials and Metallurgical Engineering

Met 426/526	Homework

A calculation for hC in a liquid steel at 1873 K results in a value of 0.8.  Calculate the wt% C in the steel if the steel contains:

- Nothing but C and Fe

- 1.1wt %Cr

- 1.1wt %Cr, 0.5 wt% Si, 0.05 wt% S, and 0.3 wt% Ni

From Introduction to Thermodynamics of Materials 3rd ed., D. R. Gaskell, Taylor and Francis, London, 2003

| for dilute solutions of elements dissolved in liquid iron at 1600 °C |
| --- |
|  | j |
|  |  | Al | C | Co | Cr | H | Mn | N | Ni | O | P | S | Si |
|  | Al | 4.8 | 11 |  |  | (34) |  | (0.5) |  | -160 |  | 4.9 | 6 |
|  | C | (4.8) | 22 | 1.2 | -2.4 | (72) |  | (11.1) | 1.2 | (-9.7) |  | 9 | 10 |
|  | Co |  | (6) |  |  | (11) |  | (4.7) |  | (2.6 |  |  |  |
| i | Cr |  | (-10) |  |  | (-11) |  | (-16.6) |  | (-13) |  | (-3.55) |  |
|  | H | 1.3 | 6.0 |  | -0.22 | 0 | -0.14 |  | 0 |  | 1.1 | 0.8 | 2.7 |
|  | Mn |  |  |  |  | (-7.7) |  | (-7.8) |  | (0) |  | (-4.3) | (0) |
|  | N | 0.3 | 13 |  | -4.5 |  | -2 | 0 | 1 | 5.0 | 5.1 | 1.3 | 4.7 |
|  | Ni |  | (5.9) |  |  | (0) |  | (4.2) | 0 | (2.1) |  | (0) | (1.0) |
|  | O | -94 | -13 |  | -4.1 |  | 0 | (5.7) | 0.6 | -20 | 7.0 | -9.1 | -14 |
|  | P |  |  |  |  | (34) |  | (11.3) |  | (13.5) |  | (4.3) | (9.5) |
|  | S | 5.8 | (24) |  | -2.2 | (26) | -2.5 | (3.0) | 0 | (-18) | 4.5 | -2.8 | 6.6 |
|  | Si | (6.3) | 24 |  |  | (76) | 0 | (9.3) | 0.5 | (-25) | 8.6 | (5.7) | 32 |

Values in parentheses are calculated from Elliott, Gleiser, and Ramakrishna using