South Dakota School of Mines and Technology

Department of Materials and Metallurgical Engineering

MET 321	Solution Tips

1.	IN - OUT + GENERATION = ACCUMULATION

(at steady state ACCUM= 0)

2.	When performing a heat or mass balance make sure you know what the balance is for.

eg:	Mass balance on O2 in a system with O, C, Fe ...
		 What species or group of species?

eg:	Heat balance "on the solid" 
		 What phase?

3.	When given problems involving rates, ratios, fractions, or percents, use a "basis of calculation" 

eg:	assume 	time = 1 minute or total mass = 100 g 
				or total moles = 100     etc

4.	Look for stoichiometric relationships.

Ex.  MxOy(S)		

If the only source of M and O is from MxOy, then
		=

5.	Mass Inputs = Mass Outputs

At steady state there is no generation of elemental mass or moles. This is also true for inert (ie non-reactive) compounds. Balances on compounds may have non-zero accumulation terms.

6.	For a system with i components there are i mass balances.  The total mass balance is redundant.

7.	Reaction Mechanisms are unimportant in overall heat and mass balances.  ∆H = State Function.

8.	Always sketch the problem.