SOUTH DAKOTA SCHOOL OF MINES AND TECHNOLOGY

DEPARTMENT OF METALLURGICAL ENGINEERING

Met 321	HQ 2	3/21/97

1)	List three methods of reducing metals from their ores.

2)	What is the slope of the PbO-PbS line on a stability diagram of Log PSO3vs Log PO2?     NOTE:  SO3 NOT SO2.

3)	What is the slope of a line of constant SO2 pressure on the above stability diagram of Log PSO3 vs  Log PO2?

4)	Sketch and Label the approximate layout of a stability diagram of  Log PSO2 vs  Log PO2 for the Pb-O-S system with the following components present: PbS, PbSO4, Pb, PbO, and PbO.PbSO4, PbO.2PbSO4, PbO.4PbSO4.

5)	In the hypothetical M-Cl2 system there are three condensed phases at 1200K: M, MCl2, MCl3.  What would be the slopes of Log PMCl vs Log PCl2  over the stable range of each of the solid phases?

6)	The roaster diagram for the Pb-O-S system would look like the sketch below.  Write the three equations which would fix the position of any one of the roaster diagram lines below.

# Text boxes

M

MCl2,

Log PMCl

MCl3

Log PCl2

100

PbO¥4PbSO4

PbO¥PbSO4

PbO¥2PbSO4

PbO

% O2

PbSO4

0

T