SOUTH DAKOTA SCHOOL OF MINES AND TECHNOLOGY

DEPARTMENT OF METALLURGICAL ENGINEERING

Met 321	HQ 2	3/24/99

- Give the general classification of each of the following reduction methods

- C + NiO = Ni + CO

- TiCl4 + 2Mg = Ti + 2MgCl2

- WO3 + 3H2 = W + 3H2O

- (Cu,xFe,yS) + (x/2+y)O2 = Cu + xFeO + ySO2

- 2Al+++ + 6e- = 2Al  while 3O2- = 1.5O2 + 6e-

2)	What is the slope of the ZnO-ZnS line on a stability diagram of Log PSO2vs Log PO2?

3)	What is the slope of a line of constant SO2 pressure on a stability diagram of Log PSO3 vs  Log PO2?			NOTE PSO3vs Log O2  NOT PSO2 vs Log O2

- Draw a silica network and show what effect the addition of a basic component has on it.

5)	On predominance diagram of the M-O-Cl system where LogPCl2 is plotted vs Log PO2,

Sketch the approximate locations of the following condensed compounds

M, MO, MO2, MOCl, MCl2, MOCl2

6)	The roaster diagram for the Pb-O-S system would look like the sketch below.  Write the three equations that would fix the position of the PbSO4/PbO•4PbSO4  line on the roaster diagram below.

# Text boxes

PbO

PbO•2PbSO4

PbO•PbSO4

PbO•4PbSO4

100

100

PbO•4PbSO4

PbO•PbSO4

PbO•2PbSO4

PbO

% O2

PbSO4

0

T

% O2

PbSO4

0

T