South Dakota School of Mines and Technology

Department of Materials and Metallurgical Engineering

Met 321	HQ 2	4/8/2005

Put all your answers on this sheet and the provided graph paper only.  Show condensed summaries of your work.  Scratch paper is allowed.

- Refer to the attached MgO-SiO2-Al2O3 (M-S-A) ternary phase diagram.

a) 	For the indicated bulk composition indicated with an “A”,

i)	What is the first crystal to appear upon cooling from the liquid state?

- What are the final three crystals when the material is completely solid?

- Characterize the system at 1900 (C.

b) 	For the indicated bulk composition indicated with an “B”,

i)	What is the first crystal to appear upon cooling from the liquid state?

- What are the final three crystals when the material is completely solid?

- Characterize the system at 1800 (C.

- Provide an example by which each of the following reduction schemes is used

  - Molten salt electrolysis (Label the sketch and show electron flow, etc..)

  - Carbothermic reduction

  - Matte Smelting

  - Metallothermic Reduction

3.	Label any five items on the below sketch of an Iron Blast Furnace.

4.	A 1050 steel (0.50 wt% C) heat at 1873 K is to be vacuum degassed.  See Data Table.

a)	If the heat has just stopped producing CO gas bubbles at 1 atm, what is the wt % O in the heat?  You may assume all activity coefficients, f, are unity.

b)	If the heat is vacuum degassed at 10-5 atm, what would the equilibrium wt % O be?  You may assume all activity coefficients, f, are unity.

5.  Derive the an equation by which the Standard Gibbs Energy value at 1873 K of the following reaction may be determined from the activity coefficient of Si at infinite dilution and the molecular weights of Si and Fe.

Si (Pure, liquid) = Si

6.	Lab Questions

a)	What value is the concept of an Assay Ton?

b) 	Where does the Pb Report (i.e. – go) during cupellation?

- Cite a basic slag component _______________ ; acid slag component _________________.

- How is Ag removed from Pb?

DATA SHEET

Data for the Pb-Zn system at 923 °K

| XZn | Zn | HMZn, Cal/gfw |
| --- | --- | --- |
| 0.2 | 4.709 | 3712 |
| 0.1 | 6.273 | 4293 |
| 0.0 | 7.94 | 4800 |

MgO-AL2O3-SiO2 Ternary Phase Diagram: attached

Data at 1600°C.   All dissolved components are in liquid iron.

+ = CO(g)			K = 500

+ 2= SiO2(g)		K = 17052

+ 2= SiO2(g)		K = 17052

H2(g) = 2H	  		K1600 = 7.3 X 10-6

log fSi = 0.029 [% Si]		MW Si = 28.09	MW Fe = 55.85

Si(1) in iron			1873K = 0.00132

∆Gvalues in cal/gmole

NaCl(l) = Na(l) + 1/2 Cl2(g)			∆G°  =  82,830

Si(1) + 02(g) = Si02 (B-quartz)			∆G°  = - 218,600 + 47.40 T

Fe(1) + 1/2 02(g) = Fe0(1)			∆G°  = -56,900 + 11.82T

SO2 + 0.5 O2 = SO3			∆G°  = -94,600 + 89.37T

0.5 O2(g) = 				∆G°  = -28,000 - 0.69T

H2(g) +0.5 O2(g) = H2O(l)			∆G°  298 K  = -57,500

Interaction coefficients for iron melts at 1873 K

e= 0.15;	e= -0.20;	e= -0.45;	e= -0.04;  Assume other fi's = 1.0

Other Information

F = 23,061 cal/v-equiv = 96,533 J/ v-equiv

R = 1.987 cal/gmole-K = 0.08205 L*atm/K*gmole

Vapor Pressure Data in atm, T[=]K:

# Text boxes

A

B