South Dakota School of Mines and Technology

# Department of Materials and Metallurgical Engineering

Met 321	HQ 3	4/29/05

1.	A vacuum-degassed steel contains 0.25 wt % carbon and 0.00001 wt % 0.  Show how to calculate the approximate pressure of CO gas in equilibrium with the melt at 1600°C.

- Assume all fC = fO = 1.

- Assume the

  - You are weary of using the pure liquid Zn as a standard state in your calculations involving the liquid Pb-Zn system and want to use the 1 wt% ss for Zn.  Show from the given data how to calculate the standard Gibbs energy change at 923 Kfor the following reaction:

Zn (pure, Liq) =

DATA SHEET

Table 1. Data for the Pb-Zn system at 923 K

| XZn | Zn | HMZn, Cal/gfw |
| --- | --- | --- |
| 0.2 | 4.709 | 3712 |
| 0.1 | 6.273 | 4293 |
| 0.0 | 7.94 | 4800 |

MW Zn = 65.37          MW Pb = 207.2

MgO-AL2O3-SiO2 Ternary Phase Diagram: attached

Data at 1600°C.   All dissolved components are in liquid iron.

+ = CO(g)			K = 500

+ 2= SiO2(g)		K = 17052

H2(g) = 2H	  		 K1600 = 7.3 X 10-6

log fSi = 0.029 [% Si]		MW Si = 28.09	MW Fe = 55.85

Si(1) in iron			1873K = 0.00132

∆Gvalues in cal/gmole

NaCl(l) = Na(l) + 1/2 Cl2(g)			∆G°  =  82,830

Si(1) + 02(g) = Si02 (B-quartz)		∆G°  = - 218,600 + 47.40 T

Fe(1) + 1/2 02(g) = Fe0(1)			∆G°  = -56,900 + 11.82T

SO2 + 0.5 O2 = SO3			∆G°  = -94,600 + 89.37T

0.5 O2(g) = 				∆G°  = -28,000 - 0.69T

H2(g) +0.5 O2(g) = H2O(l)			∆G°  298 K  = -57,500

Interaction coefficients for iron melts at 1873 K

e= 0.15;	e= -0.20;	e= -0.45;	e= -0.04;  Assume other fi's = 1.0

Other Information

F = 23,061 cal/v-equiv = 96,533 J/ v-equiv

R = 1.987 cal/gmole-K = 0.08205 L*atm/K*gmole

Vapor Pressure Data in atm, T[=]K: