South Dakota School of Mines and Technology

Department of Materials and Metallurgical Engineering

Met 321		One Weight Percent SS and Sparging Problems

1.	Compare the effectiveness of the following deoxidation methods for 100 ton steel at 1600°C, containing, initially 0.3% C and 0.006% 0.

a)	Argon sparging with 20 STP ft3/ton.

b)	Vacuum degassing at 50 mm. Hg pressure.

C + 0 = C0(g)		K1600°C  = 500

2.  Determine by calculation the maximum wt % 0 possible in steel at 1600°C containing

a)	no carbon

b)	0.20 wt % carbon

3.  How much argon per ton would be required to deoxidize a steel heat by sparging containing 0.2 wt % C to the same oxygen content achieved by vacuum degassing at 0.001 atm?  The initial heat is in equilibrium with CO gas at 1 atm.

4.  A 100-ton heat of steel at 1873 K containing 0.60 wt % C is in equilibrium with C0(g) at 1 atm.  What is the wt % 0 dissolved in the steel?

5.  How many cubic feet of argon would be required to remove 90% of the hydrogen in steel containing 0.0008 wt % H at 1773 K?

0.5 H2 (g) = H 	K1500°C = 24

6.  A 100-ton heat of steel at 1873 K containing 0.005 wt % 0 and 0.20 wt % C is to be deoxidized to 0.001 wt % 0.

a)  Can this level be achieved by vacuum degassing at 0.01 atm?

b)  How many cubic feet of argon at 298 K and 1 atm would be needed to achieve this concentration?

7.	Determine G° at 1600°C for the

Si + O2 = SiO2

For the following combination of standard states:

Si		 O2		SiO2

1wt %		1 Torr		pure l

Si(l) + 02(g) = Si02 (B-quartz)	G\s\up6(o)= - 218,600 + 47.40 T

Si(l) in iron	\s\up2(°)1873°K = 0.00132*		log fSi = 0.07 [% Si]*

MW Si = 28.09				* Hultgren et al.

H°fusion, ( -cristobalite ,high)= 2,290 cal/gmole	Tfusion,( -cristobalite ,high) = 1,996 K